## Slide 1
Designing Large Datasets: Data-Scarce and Stable Deep Generative Models for Turning Sparse Experiments into Big Datasets in Materials Science
Andreas E. Robertson
aerober@sandia.gov
Michael Buzzy, Conlain Kelly, Remi Dingreville, Surya Kalidindi
Sandia National Laboratories is a multimission laboratory managed and operated by National Technology and Engineering Solutions of Sandia LLC, a wholly owned subsidiary of Honeywell International Inc. for the U.S. Department of Energy’s National Nuclear Security Administration under contract DE-NA0003525
SAND2024-09646C

## Slide 2
Let us consider the design of a structural material for a turbine…
        We have a set of design requirements: yield behavior, expected fatigue life, stiffness, etc.
Notes: In Materials Informatics, we aim to advance our capacity to design, discover, and manufacture engineering materials.
As a field, we’ve settled on the PSP paradigm for doing this – which centralizes the importance of microstructure. The properties that define and bound our capacity to do design at the product and component length scale are defined by microstructure.
From this perspective, the study of materials very much becomes a field centralized around this idea representation. Which makes it very compatible with data science.
Over the past four years, I have studied the compatibility: developing latent spaces and representations for materials informatics – challenging because of the low data availability, high dimensionality, and complexity. The technique I have used I refer to as “algorithm hybridization” – basically studying how different paradigms produce their own latent representations and how these tools can be combined together to make up for their weaknesses and highlight their strengths.
I am going to talk about two big ones (statistics and microstructure), then I am going to talk about how we can use these latent representations to solve a application problem (design) and a technical problem (dataset development). Here, we we actual see a third latent space arise – a learned one.

## Slide 3
Let us consider the design of a structural material for a turbine…
Which alloying elements?
What grain structure?
How do we manufacture that?
Notes: In Materials Informatics, we aim to advance our capacity to design, discover, and manufacture engineering materials.
As a field, we’ve settled on the PSP paradigm for doing this – which centralizes the importance of microstructure. The properties that define and bound our capacity to do design at the product and component length scale are defined by microstructure.
From this perspective, the study of materials very much becomes a field centralized around this idea representation. Which makes it very compatible with data science.
Over the past four years, I have studied the compatibility: developing latent spaces and representations for materials informatics – challenging because of the low data availability, high dimensionality, and complexity. The technique I have used I refer to as “algorithm hybridization” – basically studying how different paradigms produce their own latent representations and how these tools can be combined together to make up for their weaknesses and highlight their strengths.
I am going to talk about two big ones (statistics and microstructure), then I am going to talk about how we can use these latent representations to solve a application problem (design) and a technical problem (dataset development). Here, we we actual see a third latent space arise – a learned one.

## Slide 4
Answering these requires expensive microstructure data in very high dimensional spaces
Which alloying elements?
What grain structure?
How do we manufacture that?
Notes: In Materials Informatics, we aim to advance our capacity to design, discover, and manufacture engineering materials.
As a field, we’ve settled on the PSP paradigm for doing this – which centralizes the importance of microstructure. The properties that define and bound our capacity to do design at the product and component length scale are defined by microstructure.
From this perspective, the study of materials very much becomes a field centralized around this idea representation. Which makes it very compatible with data science.
Over the past four years, I have studied the compatibility: developing latent spaces and representations for materials informatics – challenging because of the low data availability, high dimensionality, and complexity. The technique I have used I refer to as “algorithm hybridization” – basically studying how different paradigms produce their own latent representations and how these tools can be combined together to make up for their weaknesses and highlight their strengths.
I am going to talk about two big ones (statistics and microstructure), then I am going to talk about how we can use these latent representations to solve a application problem (design) and a technical problem (dataset development). Here, we we actual see a third latent space arise – a learned one.

## Slide 5
What characterizes valuable microstructure datasets?
Volume
Value
Reusable
Diverse

## Slide 6
These significant investments are justifiable if they can be reused.
Notes: In Materials Informatics, we aim to advance our capacity to design, discover, and manufacture engineering materials.
As a field, we’ve settled on the PSP paradigm for doing this – which centralizes the importance of microstructure. The properties that define and bound our capacity to do design at the product and component length scale are defined by microstructure.
From this perspective, the study of materials very much becomes a field centralized around this idea representation. Which makes it very compatible with data science.
Over the past four years, I have studied the compatibility: developing latent spaces and representations for materials informatics – challenging because of the low data availability, high dimensionality, and complexity. The technique I have used I refer to as “algorithm hybridization” – basically studying how different paradigms produce their own latent representations and how these tools can be combined together to make up for their weaknesses and highlight their strengths.
I am going to talk about two big ones (statistics and microstructure), then I am going to talk about how we can use these latent representations to solve a application problem (design) and a technical problem (dataset development). Here, we we actual see a third latent space arise – a learned one.

## Slide 7
The microstructure space is not well structured
Goal: Generate a statistically diverse microstructure dataset
Challenging to curate:
High dimensionality
Expensive to collect experimentally
Numerical dissimilarity ≠ microstructural dissimilarity
Requires stability (i.e., discovery)
Generated using LGD-Diffusion Models

## Slide 8
Statistical Latent representations provide the necessary stability and topology.
Microstructure Space
2-Point Statistics Space
Diversity in Statistics signals diversity in Property and Structure

## Slide 9
2-Point Spatial Statistics quantify the spatial arrangement of salient microstructure features
They are physics-driven descriptors that capture the most important microstructure information with respect to many arbitrary properties
2-Phase Microstructure

## Slide 10
2-Point Spatial Statistics quantify the spatial arrangement of salient microstructure features
They are physics-driven descriptors that capture the most important microstructure information with respect to many arbitrary properties
2-Phase Microstructure
2-point statistics of Yellow Phase

## Slide 11
2-Point Spatial Statistics quantify the spatial arrangement of salient microstructure features
They are physics-driven descriptors that capture the most important microstructure information with respect to many arbitrary properties
2-point statistics of Yellow Phase

## Slide 12
Proposed Solution: Create an intermediate dataset in the space of statistics…
2-Point Statistics Space
Sample space of 2-Point Statistics
Filtering
Synthesize 2-point statistics

## Slide 13
Proposed Solution: … then, generate a microstructure dataset
2-Point Statistics Space
Sample space of 2-Point Statistics
Local-Global Generative models to Synthesize Microstructures from statistics
Filtering
Synthesize 2-point statistics
ith pixel
jth pixel
Global Gaussian Random Field
Local Neighborhood Denoising

## Slide 14
Gaussian Process kernels provide a potential mechanism for ‘dreaming up’ 2-point statistics
Spectral Mixture Kernels

## Slide 15
We constructed four parametric strategies for placing the Spectral Mixtures
Central major axis strength, minor axis strength, angle
Volume fraction
Central major axis strength, minor axis strength, angle
Primary major axis strength, minor axis strength, radial distance
Volume fraction
Central major axis strength, minor axis strength, angle
Primary and Secondary major axis strength, minor axis strength, radial distance
Volume fraction
Major axis strength, minor axis strength
Lattice rotation, lattice spacing, lattice cutoff
Volume fraction
An overwhelming parameter space… N9 autocorrelations
a
b
θ
L
L
ψ
ψ

## Slide 16
Space-Filling reduces data set size while improving uniformity of coverage.
Subsampled to 10k Autocorrelations

## Slide 17
We generate the dataset by combining the identified autocorrelations with neighborhoods
Synthesize Microstructures
ith pixel
jth pixel
Global Gaussian Random Field
Local Neighborhood Denoising

## Slide 18
Local-Global Decomposition Models are deep generative models which systematically target physics-driven microstructure statistics
TI64 – EBSD
Nickel Superalloy – Segmented SEM

## Slide 19
Long range patterns are governed by 2-point statistics
TI64 – EBSD
Nickel Superalloy – Segmented SEM

## Slide 20
Higher order statistics characterize local neighborhoods
TI64 – EBSD
Nickel Superalloy – Segmented SEM

## Slide 21
The theoretical LGD model explicitly incorporates both sets of statistics
A Generative Framework
A global Gaussian Random Field model
Trained with just 1 training image
Combined model can extrapolate to out-of-distribution 2-point statistics.
A Local Deep Diffusion Model

## Slide 22
We generate the dataset by combining the identified autocorrelations with neighborhoods
Synthesize Microstructures
ith pixel
jth pixel
Global Gaussian Random Field
Local Neighborhood Denoising

## Slide 23
The dataset is generated by via the Local-Global Decomposition Inverse Transformation.
Generate a diverse dataset by inverting a simpler uniform distribution over microstructure statistics
Feature Diversity: Higher order statistics
Salient Statistical Diversity: 1- and 2-point statistics

## Slide 24
Efficiently covering the microstructure space also…
… yields good coverage of many property spaces.
For GRF, 1000 Contrast Ratio

## Slide 25
Specific properties can be achieved by modulating 2-point or higher statistics.

## Slide 26
Important Takeaways
Statistics guided Microstructure Dataset Construction provides achievable targets to maximize diversity in structure and property
MICRO2D is an open-source big microstructure dataset
Volume
Value?
Diverse
Reusable

## Slide 27
Materials Priors and Multi-modal Modeling
Michael Buzzy

## Slide 28
Materials Priors and Multi-modal Modeling
Microstructure Sensitive Design
Generale, Robertson, ... “Inverse Stochastic Microstructure Design”, 2024.
Michael Buzzy
Generale, ..., Robertson, ... “A Bayesian Approach to Designing Microstructures and Processing Pathways for Tailored Material Properties”, 2024.

## Slide 29
Materials Priors and Multi-modal Modeling
Nondestructive Monitoring
Rossin et al. “Bayesian inference of elastic constants and texture coefficients in additively manufactured cobalt-nickel superalloys using resonant ultrasound spectroscopy”, 2021.
Michael Buzzy

## Slide 30
Lets look at LLMs to understand challenges we might face…
Udandarao et al. “No “Zero-shot” Without Exponential Data: Pretraining Concept Frequency Determines Multimodal Model Performance”, 2024.
Generalized, multi-application and multi-modal models exacerbate the need for data.

## Slide 31
Questions?
Regression Targets:
Repeated for Low (10x), Medium (100x), and High Contrast (1000x):
  Effective Elastic Coefficients (C11, C12, C22)
  Full-field Elastic Strain
Thermal Conductivities:
  Effective Thermal Conductivities (k11, k22)
Robertson, A.E., Generale, A.P., Kelly, C., Buzzy, M., and Kalidindi, S.R., MICRO2D: A Large, Statistically Diverse Heterogeneous Microstructure Dataset, IMMI, 2024.
Andreas E. Robertson – aerober@sandia.gov
Dr. Surya R. Kalidindi – surya.kalidindi@me.gatech.edu
Adam P. Generale – agenerale3@gatech.edu
Conlain Kelly – ckelly84@gatech.edu
Michael Buzzy – mbuzzy3@gatech.edu
87,379 2D 2-phase Microstructures:
  10 Neighborhood classes

## Slide 32
Extra Slides

## Slide 33
What characterizes valuable microstructure datasets?
Volume
Value
Reusable
Diverse

## Slide 34
Synthetic microstructures match salient properties
… even without specifically targeting them in the generative model

## Slide 35
(1) “Mechanical MNIST”
(2) Process Driven Curation
Lejeune. 2020.
Zapiain et al. 2021.
t0
t10
t100
Volume
Value
Diverse
Reusable
Volume
Value
Diverse
Reusable
Available generation strategies specialize in specific characteristics

## Slide 36
In practice, the statistics and the GRF guides and stabilizes the deep diffusion model

## Slide 37
The neighborhood distributions produce diversity in higher order statistics
2-point statistics
3-point statistics

## Slide 38
The generated dataset displays greater diversity when compared to other datasets…
… such as the TAMU spinodal dataset.

## Slide 39
What’s next? It’s unlikely we have sampled everything useful passively.
Active exploration strategies and application specific targets could provide guidance.

## Slide 40
123 PC Vectors are Necessary to capture 99.9% of the Variance
The GRF Class displays the widest diversity

## Slide 41
The remaining classes cover subsets of the microstructure space because their…
… neighborhoods are restricted.