## Slide 1: Scoring Morphological Change in Computed Tomography Images of Pentaerythritol Tetranitrate (PETN)
SAND2024-09459C
Ariana Beste/ 7555, Daniel C. Bufford/ 7555,
Dan S. Bolintineanu/ 1516, Kevin M. Potter/ 5575
MLDL Workshop, September 9th -12th 2024

## Slide 2: Problem Statement
Energetic Material Surveillance
Component Shelf-life Programs
Current SEM/CT image analysis workflow
CT stack
~ 2000 2D images
Material transformation due to
thermal exposure
manufacturing defect
impurity
material incompatibility
Previously unseen changes
Traditional morphology analysis
Convolutional neural networks
Unlabeled data
Class imbalance
Unsupervised approach
Only nominal data is used
Feature Anomaly Detection System# (FADS)
# A. P. Garland, K. M. Potter, M. Smith, Feature anomaly detection system (FADS) for intelligent manufacturing, ArXiv 2022, abs/2204.10318.
Data
Desired
Realization

## Slide 3: Approach
Pretrained CNN
Morphology Scores: Feature Anomaly Detection System (FADS)
Nominal Images
“Training”
Test Images
Testing
Comparison of network activations
ResNet18
PETN powder 50% TMD
Aged for 1 to 3 weeks at 25°C, 70°C, 85°C, 100°C
MicroCT images, resolution 0.6 μm/pixel
~2000 image per scan, cropped to 1120x1120
Batches of 100 nominal and test images
Global histogram equalization
R-Vector
Difference between aggregated activations of nominal and test images per filter
Morphology score: 90th percentile of R-vector

## Slide 4: PETN CT Images
Pristine
Aged at 70°C
Aged at 85°C
Aged at 100°C

## Slide 5: Anomaly Score Variations for Images of Pristine PETN
Exchange of nominal set
1a
2a
3a
4a
Anomaly score differences due to image-to-image variations
Mean: 0.53
Std: 0.027
Sample 1a stands out

## Slide 6: Anomaly Scores with Increasing Aging Temperature
Morphological change within 1 week
Unexplained decrease in score after week 1
Onset of morphological change at 85°C
Significant morphological change at 100°C
25°C
70°C
85°C
100°C

## Slide 7: Morphological Metrics
Random walker segmentation, no filter
volume fraction (density)
specific boundary length (specific surface area)
two-point correlation function (measure of the probability that two points separated by a given distance fall within the same phase)
local thickness of the pore and particle phase (pore and particle size distribution)
Understanding and interpretation of neural network scores

## Slide 8: Volume Fraction, Specific Boundary Length
Sample 1a pressed to higher density  higher anomaly scores
Unphysical volume fraction decrease likely due to effective resolution change as PETN coarsens
1a
Onset of decrease at 85°C
Significant decrease at 100°C
Decrease due to volume fraction decrease and coarsening
Same trends as for anomaly scores
Kink in volume fraction and specific boundary length as in anomaly scores

## Slide 9: S2 Decay Length and Local Thickness
Measures of characteristic particle/pore size
Same trends as for specific boundary length and anomaly scores but less separation
Solid phase
Pore phase
Kink in S2 decay length and local thickness as in anomaly scores

## Slide 10: Conclusion
FADS to score morphological change in CT images of PETN aged at different temperatures
  Clear separation between pristine PETN and PETN aged at 100°C, onset of morphological change at 85°C
    Higher scores for sample 1a
    Initial score increase due to aging followed by a score decrease as PETN was aged beyond one week
Verification of trends and ‘outlier’ sample by visual inspection and calculation of morphological metrics
  Morphological metrics varying success in quantification of material change

## Slide 11: FADS Scores for SEM Images of PETN Pellets
Large score variations
High resolution but inconsistent imaging artefacts
Lots of noisy image data within energetic material surveillance