## Slide 1
Pranav Rane (prane@haverford.edu)
Faculty Advisors: Phillip First, Zhigang Jiang
Mentor: Alisha Vira
Characterization of Ion-Induced Damage: Application of CNNs
Image Credit: NASA

## Slide 2: Radiation Sources
Parent lattice
Modified surface layer
Intraoperative radiation therapy (IORT) can use high-energy electrons
Nuclear fission can cause irradiation of high-energy neutrons.
Nature
Human-made
SCR
GCR
EGCR
-particle
-particle
gamma ray
Parent
Daughter

## Slide 3
NASA
Burke et al. (2022)
NASA
e-
+
Solar wind: high-energy ions
H
H
O
H
O
H
H
Burgess et al. (2023)

## Slide 4
Objective: Irradiate Apollo 17 lunar sample with ions to recreate solar wind vesicle formation
SiO2
Lunar sample 75035.232
2H+ ions
Question: What fluence (ions/cm2) creates subsurface vesicles?
Atomic force microscopy (AFM)
Fluence
surface blisters
deep cavities

## Slide 5
Is the character of surface blisters correlated with the character of subsurface vesicles?
Need semantic segmentation…
Character:
Blister Coverage (%)
surface
sub-surface

## Slide 6
Semantic segmentation (U-net)
Overview:
Convolutional neural network with U-net architecture
Classification of each pixel as ‘blister’ or ‘background’
Limitations:
Small training data size → incorrect classifications
Single metric: blister coverage (%)
Results: Binary Mask
blister
background
incorrect classifications
Solutions:
Pretrained neural network
Instance segmentation

## Slide 7
Instance segmentation
semantic segmentation
instance segmentation
New metrics:
Average object area
Object number density (e.g. # of people per image)

## Slide 8
StarDist
Schmidt, Weigert et al. (2018)
3x3x128 conv + ReLU
branch 1
branch 2
1x1x1 conv + sigmoid
1x1xn conv + none
Cell centroid map ()
Radial components map ()
Pixel (i,j)
Radial Components Map

## Slide 9
StarDist Implementation
Fiji/ImageJ
Python
model.export_TF()

## Slide 10
Fluence/blister relation
Conclusion:
Spatially separated surface blisters form on SiO2 when deuterium fluence < 1018 cm-2
When fluence > 1019 cm-2 surface blisters erupt (overexposure)
1017

## Slide 11
Future work
Explore correlations between fluence and other statistical metrics such as blister number density and average blister size
Use STEM and StarDist to characterize subsurface vesicles in anorthite to confirm correlation between surface blister character and subsurface vesicle character
Use calibrated fluence to irradiate Apollo 17 lunar sample to recreate solar wind vesicles and use nano-FTIR to identify water
Lunar sample 75035.232
H
H
O
H
O
H
H
Fluence
1
2
3
4
5
6
7
8
9
10

## Slide 12
Acknowledgements
Georgia Tech Prof.
Contact: prane@haverford.edu
“17.3: Types of Radioactivity- Alpha, Beta, and Gamma Decay,” Chemistry LibreTexts. Accessed: Jul. 24, 2024. [Online]. Available: https://chem.libretexts.org/Bookshelves/Introductory_Chemistry/Introductory_Chemistry/17%3A_Radioactivity_and_Nuclear_Chemistry/17.03%3A_Types_of_Radioactivity-_Alpha_Beta_and_Gamma_Decay
U. Veronesi et al., “A preliminary report of intraoperative radiotherapy (IORT) in limited-stage breast cancers that are conservatively treated,” European Journal of Cancer, vol. 37, no. 17, pp. 2178–2183, 2001, doi: 10.1016/S0959-8049(01)00285-4.
U. Schmidt, M. Weigert, C. Broaddus, and G. Myers, “Cell Detection with Star-convex Polygons,” vol. 11071, 2018, pp. 265–273. doi: 10.1007/978-3-030-00934-2_30.
“CERN’s plans for a new particle accelerator dwarfs the existing LHC,” The Silicon Review. Accessed: Jul. 24, 2024. [Online]. Available: https://thesiliconreview.com/2019/01/lhc-successor-fcc-20-billion
K. D. Burgess, B. A. Cymes, and R. M. Stroud, “Hydrogen-bearing vesicles in space weathered lunar calcium-phosphates,” Commun Earth Environ, vol. 4, no. 1, p. 414, Nov. 2023, doi: 10.1038/s43247-023-01060-5.
C. Burke, R. L. Howard, and P. Kessler, “Internal Layout of a Lunar Surface Habitat,” 2022.
S. J. Zinkle and G. S. Was, “Materials challenges in nuclear energy,” Acta Materialia, vol. 61, no. 3, pp. 735–758, Feb. 2013, doi: 10.1016/j.actamat.2012.11.004.
“NUCLEAR 101: How Does a Nuclear Reactor Work?,” Energy.gov. Accessed: Jul. 24, 2024. [Online]. Available: https://www.energy.gov/ne/articles/nuclear-101-how-does-nuclear-reactor-work
K. Nordlund et al., “Primary radiation damage: A review of current understanding and models,” Journal of Nuclear Materials, vol. 512, pp. 450–479, Dec. 2018, doi: 10.1016/j.jnucmat.2018.10.027.
O. Ronneberger, P. Fischer, and T. Brox, “U-Net: Convolutional Networks for Biomedical Image Segmentation,” May 18, 2015, arXiv: arXiv:1505.04597. Accessed: Jul. 31, 2024. [Online]. Available: http://arxiv.org/abs/1505.04597
References